## Slide 1: Thermal Stability of LiCoO2 and Garnet Solid Electrolyte Li7La3Zr2O12

## Slide 2: Outline
Introduction/Background
Experimental Process
Results
Conclusion

## Slide 3: Motivation
To better understand the thermal
stability of the LCO and LLZO composite
Decrease the interfacial impedances

## Slide 4: Solid State Electrolytes
Solid superionic conducting material
Replaces traditional liquid electrolyte
Creates a strong ionic bridge between cathode and anode

## Slide 5: Benefits
Safety
  Boeing 787, Tesla Model S, Cell Phones, Laptops, Etc
Increased Power Density
  More battery life and charge cycles
Degeneration
  Can last thousands of years
Temperature Stability

## Slide 6: Cons
Cost to Produce
  Rare materials – Ex. Germanium
  Lengthy, in depth production methods
Interface Impedences
  Poor cycle stability
  Poor rate capability
Currently Unrealistic Applications
  Ex. Lithium-Air

## Slide 7: My Research
Different Lithium Lanthanum
Zirconium Oxide States
  Cubic
  Tetragonal
X-Ray Diffraction (XRD)
Electrochemical Impedance Spectroscopy (EIS)
Differential Scanning Calorimetry (DSC)

## Slide 8: Material Fabrication
Initial LLZO mixing
  Cubic doped with aluminum
  Ball Mill
Cold Press and Heat Sample
Grind and Store in Glove Box
Spark Plasma Sintering (SPS), XRD, Furnace Sintering

## Slide 9: Cubic LLZO Electrochemical Impedance Spectroscopy

## Slide 10: Tetragonal LLZO Electrochemical Impedance Spectroscopy

## Slide 11: XRD of Pure c-LLZO and t-LLZO

## Slide 12: XRD Analysis of Cubic Phase LLZO - LCO

## Slide 13: XRD Analysis of Tetragonal Phase LLZO - LCO

## Slide 14: Cubic Differential Scanning Calorimetry
Chart: Temp ºC
H2O
LiOH
LiZrO and LaLiCoO

## Slide 15: Tetragonal Differential Scanning Calorimetry
Chart: Temp ºC
LiOH
H2O
Lithium Vaporization
LiZrO and LaLiCoO

## Slide 16: Conclusion
Cubic LLZO is not thermally stable enough to undergo sintering
Different methods should be considered
LCO and c-LLZO could still be good product despite impurities
  Impurities may have minimal effect
  Needs further research

## Slide 17: Thank you for your time!