## Slide 1
Electrical contacts to two dimensional semiconductors
Wenjin Zhao, Tauno Palomaki, Joe Finney, Zaiyao Fei, Paul Nguyen, Frank McKay, David H. Cobden
Nanodevice Physics Lab, Department of Physics, University of Washington, Seattle WA 98195-1560
2D materials: graphene, h-BN and WSe2
The development of atomically thin layers of van der Waals bonded solids has opened up new possibilities for the exploration of 2D physics as well as for materials for applications. There are semimetals, insulators and semiconductors among them. Combining them into heterostructures offers a new route to efficient, stable and flexible solar cells. Below are the structures of graphene, hexagonal boron nitride (h-BN) and tungsten diselenide (WSe2).
Semiconductor
Structure of WSe2, with W in blue and Se in yellow
Insulator
Structure of h-BN, with B in blue and N in pink
Semimetal
Structure of graphene, a lattice of carbon atoms
WSe2 and MoSe2 hererojunction
Device fabrication
Transport measurements
WSe2 monolayer
Simplified band structure indicating circularly polarized selection rules.
MoSe2
WSe2
Triangular monolayer crystals containing lateral heterojunctions between monolayer MoSe2 and WSe2 grown by physical vapor transport on SiO2
HRTEM image by Ana Sanchez and Richard Beanland, University of Warwick
Photolumi-nescence is enhanced at junction
Lattice-perfect 2D heterojunction within a monolayer, analogous to a 3D semiconductor heterojunction
MoSe2
WSe2
Reference: "Electrical tuning of valley magnetic moment via symmetry control", S. Wu, J.S. Ross, G.-B. Liu, G. Aivazian, A.M. Jones, Z. Fei, W. Zhu, D. Xiao, W. Yao, D.H. Cobden,and X. Xu, Nature Physics 9, 149 (2013)
Reference: “​Lateral heterojunctions within monolayer semiconductors", C. Huang, S. Wu, A.M. Sanchez, J.J.P. Peters, R. Beanland, J.S. Ross, P. Rivera, W. Yao, D.H. Cobden, and X. Xu. Nature Materials (2014).
To study the electrical contacts on WSe2, we exfoliate graphene, h-BN and WSe2 on SiO2. Then we use the “dry transfer technique” to pick top h-BN and two few-layer-graphene flakes. Then we pick up WSe2 and the middle h-BN. Finally we pick up two contact gates and the bottom h-BN. We then melt the stack down onto a gold contact pattern. The result is an encapsulated bilayer WSe2 split-contact-gate device.
BG
CG
CG
Contact
Contact
Future TG
Technique: Dean, C. R. et al., Nature 497, 598–602 (2013)
h-BN
h-BN
h-BN
Gr contact
Gr contact gate
Gr contact gate
WSe2
Au back gate
SiO2/Si
Gr contact
Picture of the device
Side view of the device
A good two dimentional semiconductor solar cell requires low contact resistance. The measured resistance is the sum of contact resistance and channel resistance. We can control and measure the two resistances separately using the multiple gates.
Contacts are off
Contacts are off
Channel is off
Channel is off
T=300 K
Back gate voltage(V)
Back gate voltage(V)
Contact gate voltage(V)
Contact gate voltage(V)
Log(conductance)(μS)
Log(conductance)(μS)